AN Investigation of the use of Processed Hemp FIBER IN Digital Fabrication

by

Adam Brewer

A Thesis

Submitted to the Faculty of Purdue University

In Partial Fulfillment of the Requirements for the degree of

Master of Science

Department of Computer Graphics Technology

West Lafayette, Indiana

May 2017

THE PURDUE UNIVERSITY GRADUATE SCHOOL

STATEMENT OF CHOOSE THESIS TYPE APPROVAL

Dr. Esteban Garcia Bravo, Chair

Department of Computer Graphic Technology

Dr. Craig L. Miller

Department of Computer Graphic Technology

Dr. Kevin D. Gibson

Department of Botany and Plant Pathology

Dr. Jose M. Garcia Bravo

Department of Engineering Technology

Approved by:

Dr. Patrick Connolly

Head of the Departmental Graduate Program

Dedication

First and foremost I would like to thank God for allowing me this opportunity to achieve this obstacle in my educational career. These goals are constant reminders of all the trials and tribulations I have overcome and will face in the future. Looking back on these achievements, I will be able to face the future knowing you will not lead me astray.

This work is also dedicated to all the ones who have supported me through my educational goals. Family and friends who were giving encouraging words, phone calls, and prayers throughout this journey.

I would also like to dedicate this to the advisors on my committee that I work with to complete this task. Giving your input and familiarity in particular areas allowed for an overall collection of knowledge for an expertise understanding in this subject area.

ACKNOWLEDGMENTS

I would like to acknowledge Dr. Alton L. Kornegay for investing interest in my initiative to succeed in my undergraduate career. Having observed my efforts and approaching me with the opportunity and information to visit Purdue through the Historically Black Institutes program, I was accepted into the Master’s program in Computer Graphic Technology. Dr. Kornegay is the true definition of a professor who truly cares and seeks the success of his students. He continues to track my success, showing that I was not just another student in one of his classes. Without his observations and helping hand I would not have had this great opportunity.

I would also like to acknowledge my other professors at North Carolina A&T State University for the mental and educational preparations needed to face the world. Dr. Robert Cobb Jr., for instilling the thought, “It’s about relationships.” Dr. Cobb taught me that sometimes you have to depend on others and work as one to complete a task. There is power in numbers. Additionally, Professor Paul G. Pettie for taking the time to address needs to help me push my mental capacity for designing. Dr. Tony E. Graham, I, for preparing and helping me gain a sense of the real world by helping me address problems and not solely rely on my professors.  Without the guidance and influence of these professors, success would not have been possible at Purdue.

Finally, I would like to acknowledge North Carolina A&T State University for providing a sense of appreciation for a university focused on the success of people of color. The life lessons learned at the university put life in perspective when arriving at a Predominantly White Institute. A&T taught me how to carry myself and fight for what I want to achieve in life, despite obstacles standing in front of me. Attending a Predominantly White Institute helped me appreciate what attending a Historically Black College or University does for people of color and helping promote their success through life experiences. Being able to identify with the faculty and relate to life experiences which have molded and shaped their careers while having that knowledge passed down. Experiencing the ability to learn about your background and pursue education because it is rooted in the heritage of the university. Experiences like these that hold magnitude and influence lives of minorities and enhance their well-being to strive for success will greatly shape and influenced life.

TABLE OF CONTENTS

LIST OF FIGURES	viii

ABSTRACT	x

CHAPTER 1: INTRODUCTION	14

1.1 Research Question	14

1.2 Scope	15

1.3 Significance	16

1.4 Assumptions	18

1.5 Limitations	19

1.6 Delimitations	19

1.7 Definition of Key Terms	20

1.8 Summary	21

CHAPTER 2: LITERATURE REVIEW	22

2.1 Intro	22

2.1 Background on Hemp	23

2.2 Harvesting Hemp and Benefits	24

2.4 Current Ideals for Fibers in Industry	26

2.5 Background on OSB Board	28

2.6 How does Hemp Apply to this Study?	30

2.7 Processing of Hemp Fibers	34

2.8 Digital Fabrication	35

2.9 Usage of Digital Fabrication for Construction	36

2.9.1 Conclusion	36

CHAPTER 3: METHODOLOGY	38

3.1 Pilot Work	38

3.2 Hypothesis	42

3.3 Apparatus	42

3.4 Testing Conditions	47

3.5 Testing Procedures	47

3.6 Data Sources	49

3.7 Specific Measures for Success	49

3.8 Threats to Validity	49

3.9 Summary	50

CHAPTER 4: REVIEWING OF COLLECTED DATA	51

4.1 Preparation for Data Collection	51

4.2 Hemp Fiber Data	52

4.3 OSB Board Data	58

4.4 Comparison of Combined Data Averages	63

4.5 Comparison of Data Averages of Individual Specimens	64

4.6 Comparison of Data Averages within Categories using T-Test	69

CHAPTER 5: CONCLUSION	75

5.1 Conclusion	75

5.1 Future Works	76

LIST OF REFERENCES	77

LIST OF FIGURES

Figure 1 Seattle public Library	17

Figure 2 box for compressing fibers	39

Figure 3 top pressing fibers	40

Figure 4 pressed fiber board	41

Figure 5 Engineering Curve Aswkeland, 1994	44

Figure 6 Dog Bone specimen retrieved from Shimadzu Excellence in Science	44

Figure 7 Pull Test Diagram Aswkeland ,1994 ……..……………………............45

Figure 8 Thickness and Width of Specimens……………………………………51

Figure 9 Graph of Hemp Specimen 1..…………………………………………..53

Figure 10 Graph of Hemp Specimen 2…………………………………………..54

Figure 11 Graph of Hemp Specimen 3…………………………………………..55

Figure 12 Graph of Hemp Specimen 4…………………………………………..56

Figure 13 Graph of Hemp Specimen 5…………………………………………..57

Figure 14 Graph of OSB Specimen 1……………………………………………58

Figure 15 Graph of OSB Specimen 2……………………………………………59

Figure 16 Graph of OSB Specimen 3……………………………………………60

Figure 17 Graph of OSB Specimen 4……………………………………………61

Figure 18 Graph of OSB Specimen 5……………………………………………62

Figure 19 Comparison of Data Averages………………………………………..64

Figure 20 Comparison of Data Specimen 1……………………………………..65

Figure 21 Comparison of Data Specimen 2……………………………………..66

Figure 22 Comparison of Data Specimen 3……………………………………..67

Figure 23 Comparison of Data Specimen 4……………………………………..67

Figure 24 Comparison of Data Specimen 5……………………………………..68

Figure 25 Data information used for performing T-test…………………………69

Figure 26 T-test on peak load comparison of samples…………………………..70

Figure 27 T-test on pea stress comparison of samples…………………………..71

Figure 28 T-test on strain at break comparison of samples……………………...72

Figure 29 T-test on modulus of GPa comparison of samples……………………73

ABSTRACT

Author: Brewer, Adam MS

Institution: Purdue University

Degree Received: May 2017

Title: (An Investigation on the use of Processed Hemp Fiber in Digital Fabrication.

Major Professor: Esteban Garcia

The world of hemp has been around for centuries, and now the industry (bio-composites, construction, among others) are shedding light on the possibilities that hemp provides in multiple areas. Hemp fibers are one of the strongest fragments of a hemp plant and can be processed in a fashion that can be used in different applications. The fibers also possess the qualities of an environmentally friendly material. Through incorporating the use of technology through digital fabrication, can hemp fibers be digitally fabricated and still possess the qualities to be used in industry?

Comparing the hemp fibers that will be made up to replicate the form of prefabricated OSB (oriented strand board), tests will be performed to create an engineering curve and display data collected in four areas. The four areas of data collection will be peak load, peak stress, strain at break, and modulus of GPa. The data results were compared in each category using a T-test to see if any significant difference were shown.

CHAPTER 1: INTRODUCTION

This chapter establishes grounds for the completion of aresearch study on the use of digital fabrication of hemp fibers for use in industry. The research was accomplished through the description of a significant problem within this area and was further distinguished by the boundaries in which the study was performed.

Looking further into the industry and demand for new materials, can hemp fibers be manipulated by digital fabrication and still possess qualities for industry standards? Conducting research within this area, hemp fibers stood out over other materials. The factors that lead to this were attributions such as green properties, strength, and ability to replace timber. Since the industry is focusing on the use of green materials, the research on hemp fibers continued, and results were concluded that hemp fibers are an abundant candidate for the material used in this study.

Next, the most important question is the ability to manipulate the hemp fibers in a manner in which digital fabrication can be applied through the use of technology. Conducting tests and looking at ways to manipulate this material to be used in industry, the study lead to a depth of research and discoveries. The research enclosed in this thesis discusses literature and references based on this study to conclude if hemp fibers may be a sustainable product to use when digitally fabricated for use in industry.

1.1 Research Question

This research was based in the area of industrial materials and the use of digital fabrication on hemp fibers and their ability to still house industry qualities. Industrial material usage being an area that is gravitating towards green materials, the research focused on this area and hemp fibers as a possible material to use in industry. By incorporating the use of digital fabrication, this research determined if the fibers surpassed the measures of a prefabricated OSB board. The research question that was explored was: Can the digital fabrication of hemp fibers prove significantly better than prefabricated OSB board in terms of peak load, peak stress, strain at break, and modulus of GPa?

1.2 Scope

Engaging in research pertaining to the use of materials being used within the industry, the researcher discovered that industry is always looking for sustainable materials to be used for new products. The use of hemp fibers may be a solution to some of the problems being faced when looking within this area: addressing needs for green materials, less consumption of trees, and the ability to digitally fabricate hemp fibers through digital manipulation, among others. “Hemp fibers are one of the most valuable parts of the hemp plant. It is commonly called bast, which refers to the fibers that grow on the outside of the plant’s stalk. Bast fibers give the plant its strength.” (Hemp Fibers, 2016, para.1)

So how can the use of hemp fibers help address this need of new materials for the industry? The solution that this study proposed was to digitally fabricate hemp fibers to use while keeping industry standards when compared to prefabricated OSB board. Digital fabrication is a type of manufacturing process where the machine used is controlled by a computer. “The most common forms of digital fabrication are CNC Machining ( Computer Numerical Control); where shapes are cut out of materials, 3D Printing, or Laser-fabricated” (Open Desk, 2016, “What is digital fabrication,” para. 1).  The process will involve creating a board for testing which is composed like oriented strand board (OSB). By laying thin particles of wood across each other and then compressing them to make one complete board, an OSB board is formed. These samples were used to conduct tests for peak load, peak stress, strain at break, and modulus of GPa. This data was compared to the characteristics of OSB board as a standard guideline because the composition of both of these materials are closely comparable.

1.3 Significance

When investigating the aesthetics of contemporary architecture and the materials being used to achieve these designs, the reader must first understand the breadth of the terms that are being used to explain the process. Contemporary architecture is defined in broad terms - the architecture of the present day. “The term contemporary architecture is applied to a range of styles of recently built structures and space that are optimized for current use while incorporating unique designs” (Barrett, 2014, “What is contemporary architecture?” para. 1). Contemporary architecture is the most relevant way of designing for architecture pertaining more to public spaces than personal spaces. The design process has no limits and can take on features that can prove to be very difficult to achieve for the constructors. The proposals are no longer designed with the concepts of modern architecture, which were defined styles and used since the mid-19th century.

Figure 1. Contemporary Architecture Seattle Public Library

The next question about this research was, why this work is important in the world in which we live today? Considering this research from a contemporary architecture discipline, if the research is successful, hemp can be viewed as a material choice for more complex designs in this industry. The architect would now be able to achieve designs that will be more abstractly sound, created in ways that the spectator is engaged in the form of the design.  This can be aesthetically pleasing to the viewers and also be in tune with the environment in which it is placed, such as using the sun to cast shadows to create a sense of depth when engaging. This would also allow the designer to design a little more freely, instead of being limited due to the materials used constricting the design features.

Another standpoint can be taken by the community in which the design will be incorporated. Hemp fibers are a green product, which means they are environmentally friendly as implied by Dittenber:

Compared to most synthetic fibers, natural fibers are low-cost, are easier to handle, have good specific mechanical properties, and require only around 20–40% of the energy production. Using natural materials and modern construction techniques reduces construction waste and increases energy efficiency while promoting the concept of sustainability. (Dittenber et. al., 2012, p. 1419)

The use of hemp fibers can be used to help design aspects in the world of contemporary architecture, which has been restricted because of the boundaries of materials being used to date. Using the technology of digital fabrication will overcome this obstacle, allowing for more complicated designs to be completed. Because the industry is moving into an era in which the environment has become an important issue, hemp fibers possessing many beneficial qualities could be used as a new material.

1.4 Assumptions

The following assumptions were inherent in the pursuit of this study:

- The use of hemp fibers to help achieve complicated designs within the industry.

- The use of hemp fibers could be used as a green material for industry.

- Hemp fiber is a green material that will benefit construction.

- Digital fabrication allows completion of complicated design aspects within the industry.

- Hemp fibers will be molded and digitally fabricated to show the manipulation of fibers are possible.

1.5 Limitations

The following limitations were inherent in the pursuit of this study:

- The amount of time to produce the digital fabricated parts to complete projects within a feasible timeline.

- The amount of adhesive needed for the hemp fibers to properly adhere for digital fabrication.

- The access to a CNC machine to be used by the designer for digital fabrication of hemp fibers.

- The amount of elapsed time for curing samples after compression has concluded.

1.6 Delimitations

The research was delimited to:

- This project will only focus on laser CNC digital fabrication.

- The cost and quantity of hemp fibers used within this project.

- This project will only focus on hemp and OSB board.

- If data results are due to resin content when combined and compressed  with fibers or natural characteristics of fibers alone

- The use of prefabricated OSB board used in testing to be compared to handmade hemp fiberboard

1.7 Definition of Key Terms

Digital Fabrication - a type of manufacturing process where the machine used is	controlled by a computer. The most common forms of digital fabrication are CNC	Machining: where shapes are cut out of wooden sheets, 3D Printing, and Laser	Cutting. There is a huge range of digital fabrication techniques. The important	aspect that unifies them is that the machines can reliably be programmed to make	consistent products from digital designs. (Open Desk, 2016, “What is digital	fabrication,” para. 1)

Hemp Fibers - are one of the most valuable parts of the hemp plant. It is commonly called	bast, which refers to the fibers which grow on the outside of the plant’s stalk. Bast	fibers give the plants strength. Hemp fibers can be between approximately 0.91 m	(3 ft.) and 4.6 m (15 ft.) long, running the length of the plant. (Hemp Traders,	2016, Hemp Fibers, para. 1)

OSB (Oriented Strand Board) - is an engineered wood-based panel consisting of strands	of wood which are bonded together with a synthetic resin; the strands are pressed	together in layers. In the outer layer’s strands are generally oriented longitudinally	in line with the panel length, whereas in the middle layers strands generally lie in	a cross wise direction. (osb-info, technical information sheet)

1.8 Summary

This section has covered the question that will be researched and the reason for research to be conducted. The article also included definitions of key terms and associated assumptions and limitations.

CHAPTER 2: LITERATURE REVIEW

2.1 Intro

When looking at materials that are sustainable, natural fibers are among the top candidates in this category. While conducting research on hemp fibers, the fibers house many qualities that deem the fibers as one of the top choices. Using composites within the industry is the new area in which material development is undergoing experimentation involving environmentally friendly composites. In lightweight composites containing hemp hurds, the author states that “Trends in research and development of environmentally friendly composite materials are focused on the “green approach” moving from the limited and non-renewable limited material resources to easily renewable raw material resources.” (Stevulova et. al., 2013, p.69) Understanding the way the fibers impact the environment, are harvested, and the usage of fibers throughout history influence the use of the fiber today. Having so many qualities and looking at the fibers for use in industry, they must be tested along with a baseline. Using a prefabricated OSB board, the test results were measured. The history of OSB will be briefly addressed to give a sense of orientation and composition of OSB board.

Considering ways to incorporate technology, we will look at digital fabrication. The use of a CNC laser machine will allow for precise designs since the device creates the designs based off of algorithms or better known as computer codes. We will first go in depth by looking at the history of hemp.

2.1 Background on Hemp

Hemp is related to the plant Cannabis Sativa and has been used for various reasons throughout time. “Known as one of the oldest textiles used, it dates back to twenty-seven centuries before Christianity” (Ash, 1948, p. 158). Mainly grown across seas, there have been many applications, which range from making rope, clothing, industrial and many environmental purposes. Despite the multiple beneficial uses, many people have the misconception that hemp is also marijuana, which is not the case. Research by West states, “The THC levels in industrial hemp are so low that no one can get high from smoking it. Moreover, industrial hemp, while low in THC, is high in another kind of cannabinoid, CBD, which counteracts THC’s psychoactivity” (West, 1998, p. 3). Having a low content of THC is also backed up by statements from Industrial Hemp in North America: Production, Politics and Potential stating, “Nevertheless, since 1990, dozens of countries have authorized the licensed growth and processing of “industrial hemp” (cultivars with quite low levels of THC)” (Cherney et. al., 2016, p. 1). One of the most promising properties of hemp is the strength of the fibers. Shahzad states:

The use of hemp fibers as reinforcement in composite materials has increased in recent years as a response to the increasing demand for developing biodegradable, sustainable, and recyclable materials. Hemp fibers are found in the stem of the plant which makes them strong and stiff, a primary requirement for the reinforcement of composite materials. (Shahzad, 2012, p.1).

Strength is an extended attribute of hemp fibers that has been proven and attested to many uses for various reasons.

2.2 Harvesting Hemp and Benefits

Hemp is known as a natural fiber and can be grown with little to no effort on the producer’s part. Hemp’s ability to grow quickly and be harvested in a quick turnaround time is a beneficial factor of hemp for use in industry. Capacity to plant hemp and cultivate the produce in a period of seventy to ninety days after seeding, (Fortenbery et. al., 2004, p.99) also benefits the agriculture land that it is planted. As implied by Ranalli:

Hemp provides many benefits, i.e. weed control, pest and disease resistance, pesticide elimination without the disadvantages, soil improvement by means of crop rotation. These agricultural benefits make hemp a suitable crop for both conventional and organic farming procedures, able to provide high biomass production with low inputs. (Ranalli, 1999, p. 2)

Using the current average rainfall projection of the US, from the high of 63.7 inches to the low of 30.21 inches, (Average Annual Precipitation), “hemp only needs to consume about 27 inches per annum” (Ash, 1948, p. 158). When the hemp has been first planted the average of about “14 inches of rainfall is needed in order for the seeds to germinate within the first six weeks” (Fortenbery et. al., 2004, p. 100).Hemp consuming less than the average low of rainfall across the U.S. would enable the crop to be planted on the majority of the land, taking into consideration the climate of the seasons.

About to the ability of hemp aiding the area in which it is planted, erosion problems could vastly be cut in half or ended. Ash implies, “The root of the hemp plants are vastly rooted deep in the ground keeping the soil intact, which would reduce erosion of the fields” (Ash, 1948). The roots deeply grounded allows for the nutrients within the ground to stay present, allowing the farmer to rotate crops the following year. The property of repelling insects is also another factor when looking at the growth of hemp for harvesting. Hemp repels insects. Thus the use of pesticides is almost obsolete. The plant also controls the growth of weeds in the area in which it is grown. These attributes are referenced in Feasibility of Industrial Hemp Production in the United States Pacific Northwest and Opportunities for Commercial Hemp Production. (Ehrensing, USDA 2000, p. 16 – 17)  Fortenbery also states, “When grown for fiber, hemp is very competitive with weeds and requires little, if any, herbicides.” This statement is also reinforced by the declaration, “Ehrensing argues that weed suppression with minimal pesticide use may be one of the greatest agronomic and environmental benefits of hemp, making it a good rotational crop.” (Fortenbery et. al., 2004) While possessing all these great qualities for the land used to plant the hemp, harvesting is only a six-step process. These processes involve chemical defoliation (removal of unnecessary leaf mass with chemical use), cutting, retting, baling, loading, and transporting as referenced in Industrial Hemp as an alternative crop in North Dakota. (Kraeznel et. al., 1998) The process of obtaining the hemp hurds is a little more vigorous, including special tools needed for the hemp hurd extraction. Usually, after transporting, the stalks are left to dry, then crushed, and then hurds are processed as stated:

After harvesting, hemp stalks are dried and then crushed (usually with a hammer crusher). The rods are then defibrated, cut and calibrated to obtain hemp hurds. The hemp hurds are partly composed of cellulose and can hold from 44 to 55% of the dry mass of the hemp stem. (Vignon et al., 1995).

The process of obtaining the fibers from the hemp stalk could prove to be timely and costly if the proper machinery is not used. “When harvesting the stalk to obtain the fibers, keeping the stalks in a parallel position allows for more precise recovery of the long fibers” (Ehrensing, D.T., 1998, p. 18). This factor is taking in consideration when the equipment used to harvest the stalk is elected. Using proper equipment helps yield longer fibers, used more readily in textiles.

2.4 Current Ideals for Fibers in Industry

Fibers are starting to be looked at for filling material gaps in many industries because of the green properties and sustainability when compared to other fibers.  In Fully Biodegradable Natural Fiber Composites from Renewable Resources states, “Compared with conventional glass fibers or carbon fibers, plant fibers have many advantages like renewable, environmentally friendly, low-cost, lightweight, high specific mechanical performance” (Zhang et. al., 2005, p. 2515)  One of the biggest uses that natural fiber composites are noticeably taking on are in the industry of car manufacturing. With hemp grown mostly across seas because of government regulations, the European countries are taking advantage of the properties of the industrial hemp fibers. The use of industrial hemp fibers has found a place in the automobile industry, “In Europe, the uptake of natural fibres in the automotive market has accelerated from 400 tons in 1996 to 17,140 tons in 2000, predicted to increase to 60,000 tons in 2005, with the greatest increases for hemp fiber” (Plackett, 2002).  Hemp’s use in industry and utilization in the automobile industry is also stated in Fibre Properties and Crashworthiness Parameters of Natural Fibre-reinforced Composite Structure stating:

Recently, natural fibres have drawn the interest of researchers, engineers and scientists as substitute reinforcements for fibre reinforced polymer (FRP) composite tubes. Due to their fairly good mechanical properties, low cost, high specific strength, environmentally-friendly and bio-degradability, ease of fabrication, and good structural rigidity, these materials can be used in an extensive range of applications, including aerospace and the automotive industry. (Alkbir, M. F. M., et al. 2016, p.59)

Natural and Wood Fibre Reinforcement in Polymers reiterates this statement listing several applications of natural fibre in the automobile and other areas where it can be used as a composite. (Bell, 2012, p. 28-29)

Natural fiber composites process many traits allowing the fibers to be good alternative candidates in many areas, including the construction field as new material. One of the most important features is the strength of the fibers, but there are others traits which are necessary for this area such as: being lightweight, electrical resistant, chemical resistant, fire resistant, moisture resistant and highly durable to name a few. Natural fibers can replace many materials that are not composed of renewable resources.

Using composites within the industry is the new area in which material development is undergoing experimentation involving environmentally friendly composites. In lightweight composites containing hemp hurds, the author states, “Trends in research and development of environmentally friendly composite materials are focused on the “green approach” moving from the limited and non-renewable limited material resources to easily renewable raw material resources” (Stevulova et. al., 2013, p.69) Since the fibers are loose when received the ability to manipulate the fibers is another consideration to take in, the ability to alter the material to fit the design needs. (Ticoalu et al., 2010, p.1)

While fibers process the greatest amount of strength, the fibers alone cannot support loads. Therefore the use of resin is used to form the composite. The resin also serves as a protector for the strands of fibers, helping preserve their trait of having strength. Using the different variables fibers can be manipulated to obtain the proper composition to complete the job. This can be achieved by controlling the amount of resin used, and in combination with the length of fibers, in conclusion, these two factors determine the composite strength.

Fibers have been used in structural and infrastructure projects where loads are being placed which are known as load bearing. The use of these fibers is implemented either with the use for rehabilitation of current structures or in the redesigning of new structures.  The application of the fibers has been used in items that such as beams, pedestrian bridges, and multipurpose panels. All of these elements are tested based on bending, “Tested for their flexural capacity with three or four points bending test will give results of load capacity, flexure stress, strain, deflection, and modulus of elasticity” (Ticoalu et al., 2010, p. 3). Structural designs are tested more along the lines of strength, which are composed of bending strength, bending stiffness, tensile strength, and tensile stiffness.

2.5 Background on OSB Board

Orientated Strand Board has been used within the industry as a substitute for other construction materials for many years.  The increase in need of OSB board has been called upon for use in the industry, “A substantial increase in production and consumption of oriented strand board (OSB) has taken place in various parts of the world over the past two decades” (Kruse et. al., 2000, p.270). OSB board is made up of wood chips, or waste materials left over and laid in particular orientations and pressed by a resin binder to create a complete board. As stated in U.S. Patent No. 3,164,511 Orientated Strand Board.

The invention relates to a structural board consisting of generally straight wood strands and a suitable binder. The wood strands may be embedded in a matrix of cement, such as Portland cement, gypsum or magnesite cement, or any one of a number of suitable synthetic resins. Each of the structural boards formed in accordance with the present invention is preferably composed of a plurality of strand-like straight wood shavings or strands suitably bonded together. “The strands each consist of a multiple numbers of the fibers of which wood is composed, the fibers being in the same position with respect to one another that they occupy in the original wood. (Elmendorf, 1965, p. 5).

When looking at the wood chips used within the OSB, some specifications are met to be used to create the board. There are length and width requirements, the average length and width are ½” to six inches and “the thickness ranges from 0.002 to 0.020 of an inch. The uses of improper wood chips would cause defects within the board” (Elmendorf, 1965, p. 9).

The OSB board outer layers are held together by resins that are composed of synthetic resins or protein-based binder. “The strands that make up the outside of the OSB board are known as the lamina, where the resin is applied either as a dry or liquid adhesive” (Elmendorf, 1965, p. 6). The inner chips or wood are bound with another type of resin.  U.S. Patent Application No. 11/794,333 states that resin is composed of,

A resin composition comprising urea and formaldehyde, whereby the resin composition further comprises melamine and/or an aromatic hydroxyl compound, wherein: the molar ratio of formaldehyde to the sum of melamine and the aromatic hydroxyl compound lies between 8:1 and 100:1; the molar ratio of formaldehyde to the sum of (NH2)2 and the aromatic hydroxyl compound lies between 1:0.2 and 1:2 (Nusselder et. al. 2006, p. 1-2).

Using the prefabricated OSB board as a base guideline to test the handmade hemp fiber boards against, will reveal if the hemp fibers are suitable for industry standards.

2.6 How does Hemp Apply to this Study?

How does the use of hemp fibers fit into the major portion of this study? Hemp fibers are part of the plant that is derived from the stalk. The industry is now focusing on the use of green materials and renewable resources to use within in different areas, but the study will be narrowed down to construction. This statement is backed up by Mora,

To build sustainable and affordable housing for the future, it is advantageous to create links between agriculture and the construction industry. Sustainability can only be possible when construction uses renewable materials, or materials recycled from construction wastes. (Mora, 2007, p.1331).

Using the hemp fibers in the construction for architecture, strength would be considered the number one is an asset having a tensile strength of about 800 MPa as referenced in the work of Thygesen. (Thygesen, 2006, p.64) Hemp is one the strongest and stiffest natural fibers available on the market, which makes it a great candidate for composites as referenced in Feasibility Study for NZ Hemp Fibre Composites (Pickering Kl et al., 2005, 15-20). Could other qualities of hemp fibers be taken into consideration when being looked at for a material to use? The trait of being a renewable resource has been listed. However what about the ability of this natural fiber to help in areas of the global energy crisis and ecological risk? These fibers could be used as a replacement for artificial fibers, “Plant fibers reinforced polymer composites have attracted more and more research interests owing to their potential of serving as an alternative for artificial fiber composites” (Bledzki et. al., 2002, p.3) The majority of the artificial fibers used in industry today is fiberglass and carbon fibers which could be devastating for the environment. The artificial fibers are also known for their brittle trait when subducted to impacts. The natural fibers show promising traits, “Compared with conventional glass fibers or carbon fibers, plant fibers have many advantages like renewable, environmentally friendly, low-cost, lightweight, high specific mechanical performance” (Zhang et. al., 2005, p.2514). The practice of using natural fibers dates back as early as 1989 as stated by Riedel.

The DLR Institute of Structural Mechanics developed an innovative idea in 1989 by embedding natural and near-natural reinforcing fibers, e. g. flax, hemp, ramie, cellulose, etc., into a biopolymeric matrix from cellulose, starch or lactic acid derivatives, etc. (thermoplastics as well as thermosets), new fiber reinforced materials, called biocomposites, were created and are still being developed. (Riedel, 1999, p.3)

Natural fibers are now making way, being observed for uses in other industries. The qualities of the fibers are being tested for different applications.

This practice has occurred throughout history for some time but has recently found its way into the construction industry in the form of hemp Crete. “Hemp Crete” is drawing considerable attention among do-it-yourselfers for its thermal properties, low cost, and ease of use.” (Pollitt, 1996, p.2)   This material is used in the same format as concrete within the design aspect of the building. The Hemp Crete is a stronger, lighter, but more sustainable material than concrete:

There are also advantages to using hemp within construction.  The biggest factor is that is a low impact factor in the environment. During photosynthesis, the hemp plant absorbs carbon dioxide from the atmosphere during the day, converting carbon to biomass and exhaling oxygen. When the hemp is subsequently used in construction, the carbon within it is locked away for the life of the building. Therefore, using hemp within the structure of a building can be better than zero carbon, sometimes referred to as carbon negative. (Bell, 2012, p.3)

The materials which make up the hemp crete allow for mechanical properties that are different from concrete used in the area of construction today. According to Li et. al.:

Hemp fibre is a good reinforcement material because it has a high tensile strength and it has a strong tolerance to alkaline environments. Due to the low density and high porosity of the hemp shives, the combination of hemp and a cementitious binder creates a building material with mechanical, thermal and acoustic properties that differ from those of conventional concrete. (Li et. al., 2006, p.497-498)

Using different properties of the lime used in the mixture such as hydraulic and hydrate allows for the mixture to be used to construct walls and reinforce wood load bearing structures within the walls in construction. Depending on the way the mixture is manipulated it can also be used in floors and roofs as spoken about in Physical Qualification of Construction Materials Based on Hemp. (Arnaud et. al., 2001, 50-56).

Using this material, the use of trees will be reduced for the materials used in the construction. The yield percentage and growth time of hemp can replace or at least slow the processing of forest for construction usage. Using references from earlier in the research, the growing time can vary from 90-120 days, only needing an average of 27 inches of rainfall per annum. Depending on the area of planting, the fibers can be harvested two to three times a year. Bell supports this statement by describing the production of hemp in the UK.

Globally there is also growing pressure to protect our tree stock for ecology as well as its importance in regulating the climate. Although timber in the UK is from managed forests, it still undergoes a relatively high amount of processing. If hemp were to be substituted for timber ‘as a tree-free fiber source, it could reduce harvesting of primary forests and the threat to associated biodiversity. Hemp ‘yields four times more fiber per acre than trees do and as Woolley states, only 1% of the agricultural land in the UK would be needed to produce enough hemp for all the new dwellings built each year. (Bell, 2012,p. 4)

Hemp having the possibility of helping slow the consumption of timber for use in construction while improving the ecology and regulating climate benefits construction and the environment.

Another factor of using hemp is that the product is biodegradable. If the building or design in which the material has been used is ever deconstructed and material is left behind, the environment would not be left to suffer because hemp is a natural product, and can be broken down naturally. Hemp fibers also process qualities which are naturally ingrained in the plant, such as mildew resistant, heat resistant, and strong as referenced in the background on hemp.  These traits are another reason hemp could be a sufficient alternative in the construction field.

2.7 Processing of Hemp Fibers

There are two types of fibers which are taken from hemp stalks. Having two bast fiber types, the long fibers have characteristics of soft woods where short fibers have consistent characteristics of hardwoods. Using processed fibers increases the strength of the fibers. There is a process in which the fibers are harvested with equipment suited for the job. The improper tools will lead to equipment failure because the fibers will bind up the equipment. The area of processing was referenced earlier in 2.1 Background on Hemp and can be referenced in Industrial Hemp as an Alternative Crop in North Dakota and Steam explosion of woody hemp chènevotte. (Krenzler et. al., 1998)

2.8 Digital Fabrication

Digital fabrication is the use of a computer that controls a machine in which material is removed from or added to a form by the use of code. The computer reads the code and performs addition or subtraction of material through detailed functions. Using the computer to remove material is a precise method that allows formed angles to be cut with little to no room for error as implied in Opendesk. “There is a huge range of digital fabrication techniques. The important aspect that unifies them is that the machines can reliably be programmed to make consistent products from digital designs” (Opendesk, 2016, What is Digital Fabrication?, para. 2). Digital fabrication can be a valuable asset to the design process within contemporary architecture because the design is now being completed using computer software. The issue within this is that sometimes the designs are so abstract that they may not be able to be constructed with materials that are available within the world of architecture. This means that the design may have to be revised or changed to complete the design. On the other hand, if the construction of the design can be completed, what will be the lifespan of that particular part of the design depending on the material that was used to complete that portion? The weight of the design aspect must be taken in consideration like the way the domes of the Roman period were designed. The weight of the domes used in Rome had to be evenly distributed as described in by Szalapaj. “The digital integration of specialist design information is concerned with how environmental aspects can be modelled and supported digitally, such as 3-D models” (Szalapaj, 2014, p.3). The contemporary architecture has taken a lot of influence from Biomimicry, using nature to influence the design. These designs usually have extruding features that are represented within the design. Some these designs can be noted in Dives in Misericord Church, Falling house, Milwaukee Art Museum, and The Eastgate development to name a few.

2.9 Usage of Digital Fabrication for Construction

The CNC uses a code to create the mold which is very precise. The code that is loaded in the program to give the CNC machine the paths that it will cut are produced in computer molding software’s. These software’s are graphic based which allows for the user to draw two dimensional shapes, then extrude, bevel, fillet, and manipulate them in several different forms. Since these software’s use codes to help produce the design or forms of the user, they will be accurate and precise when loaded in the CNC machine to be processed. This course is possible because of the graphical user interface of the programs (GUI). “Ivan Sutherland developed GUI which is known as a graphical user interface in 1963 as stated in Code + Form” (Reas, 2010, p.44). With the technology of coding increasing, the new methods of using coding included producing forms through printing and fabrication. Coding is being used in 3-D printers, CNC machines, laser cutters and many other forms. The language that the computer understands, produces the form, whether it is from a 3-D printer or CNC machines. With this new technology and applying it to use in contemporary architecture, the designs can reach and achieve more precise and complicated designs to enhance the user’s experience.

2.9.1 Conclusion

Looking at a brief background of hemp and the characteristics that the fibers derived from the stalk possess, there is better understanding of the potential of this plant. Understanding the process of growing and harvesting these fibers to ensure a high quality fibers to be used for innovative ideals in industry, while discovering new ones. Observing ideals of how the fiber can be tested in order to be used for new ideals and their ability to be manipulate to achieve workability for the user. Through the use of digital fabrication data will be collected to see if the fibers also show promising benefits for use in construction, while incorporating environmental friendly benefits. This data will be compared to see if the fibers are a replacement material for use in industry.

CHAPTER 3: METHODOLOGY

3.1 Pilot Work

After doing some research and searching for hemp board, the discovery was made that the manufactured boards are extremely expensive and hard to find. Conducting more research on hemp hurd and hemp fibers, the researcher located a company in North Carolina which sold hemp fibers. The fibers are the strongest portion of the plant and the most valuable. Using these fibers and constructing a board similar to oriented strand board (OSB), testing will be conducted to see the similarities between the two which consist of proportional limit, elastic limit, yield point, ultimate stress point, and breaking point. The researcher purchased ten pounds to begin processing material for the research. After receiving the product, further research was done on how to hold the product together and compress it for maximum consistency.

The two products in which the first pilot works were performed involving Titebond Ultimate III wood glue and Dap Weldwood Contact Cement. There was a structure created which consisted of boards that were constructed to make a 4”x6” rectangle with a depth of approximately three inches. Boards were also cut, one to cover the complete bottom of the structure and one to fit into the top of the structure used to compress the material. The structures were held together by Surebond Woodstik glue sticks. The structures were encased with the glue so the material would not be able to escape the corners of the structure to ensure proper saturation and compression. The material was then placed within the structure after an aluminum foil layer of the wrap was added so the material would not stick to the structure. After the material was added another wood plate was added, and then clamped down to compress the material. The structure was allowed to cure for 24 hours minimum to ensure complete drying time with the outcome to be observed afterward.

Figures from the process:

Figure 2. Box for compressing fibers

Figure 2 shows a mockup of the structure in which the fibers were placed. Each component is labeled. As stated this was a pilot work in which testing was done to see the possibilities of the hemp fibers, and there was no particular reason for the two types of glue chosen other than they are used to complete wood projects. The completed saturation was necessary, so the fibers will bond completely with each other.

Figure 3. Top pressing fibers

Figure 3 shows the placement of the upper part for compressing. It is important to remember to use a material that will not stick to the fibers such as a release paper; aluminum foil will work the same as the release paper. The aluminum foil allows for the fibers to be removed from the structure without any force. Placing the fibers on top of the aluminum foil and having a consistent thickness within the structure is important.

Figure 4. Pressed fiberboard

Figure 4 shows the release of the top for pressing and the fiberboard, which was the result.

After the elapsed time had passed, the materials were examined. The fibers bonded firmly together and created a board which was about a quarter of an inch thick. The consistency of the fibers was found in both of the materials, which used different bonding agents. With further testing, the boards revealed that also have a tendency to be more flexible than the standard OSB board. This observation was conducted by the simple task of flexing the board by the hand, and it retained its same after moderate flexing. Another exhilarating discovery was the fact that the boards could also be sanded without the fibers flaking. This is the opposite with the OBS board as the wood chips began to splinter after moderate sanding. With this pilot, work conducted by the researcher began to look at applications within architecture in which the fibers could be utilized while applying technology.

3.2 Hypothesis

The use of hemp fibers combined with a state such as oriented strand board will be stronger, sustainable, and could be used in industry. The researcher was looking for a significant difference, in three of the four test in the materials to deem the hemp composite boards are more sufficient. Using a T-test with a standard power of 0.05 revealed if there is a significant difference in the two materials. Using this material in digital fabrication can help create unique designs required to keep up with the demands of a changing industry.

3.3 Apparatus

Processes for the use of hemp fibers in this research were very precise to ensure all testing is within a controlled environment to ensure accurate data. The weight of the fibers was controlled. The weight of the fibers used were 75.3 grams; this weight was determined by some fibers to fill the structure completely. The same method used in the pilot work will be applied to create the fiber composite board. A new structure will be built to use for the fiber composite. The fibers were saturated and worked into the structure after the application of aluminum foil had been applied to the bottom and sides to prevent bonding with the structures. After the fibers had been placed within the structure, another application of aluminum foil was added to prevent bonding with the top portion of the structure used to apply level pressure to the fibers. A piece of ¾” 1080 steel was cut out to insert into the top of the container. This ensures that proper compression is dispersed across of the fibers. Clamps were also added to the ends of the container to ensure expansion did not occur once pressure was applied. Using a ten-ton press, 4000 tons of pressure was applied to the ¾” 1080 piece of steel. The press was checked every thirty minutes, and the pressure was applied back to 4000 tons in case pressure had dropped for a time frame of two-hour was essential to keep constant pressure. Once the time had elapsed, the fibers were removed and baked at 200 degrees for five hours to help cure out moisture.

The next step involved taking the fiberboard composite and planning it to the approximate thickness of a 1/8”, which is the specifications of the thickness of the dog bone for the ASTM (American Society for Testing and Materials), D638 test procedure. Once the approximate thickness of a 1/8” had been achieved, it was checked with a digital caliber ensured the thickness so the next step could be approached. This depth allows for test results to be compared from other testing samples under D638 guidelines.

The fiber composite board was laser cut using the template that is used to measure engineer curve and create a stress-strain diagram through the pull test of a dog bone. The engineering curve (test strain curve) is a method that can be used to show the characteristics of the test results to be analyzed and compared alongside the other test to see any variations or outliers that will be significant to the success or failure of this study. “Test data obtained by this test method are relevant and appropriate for use in engineering design.” (Standard, A. S. T. M., 2010, p.46) Figure 5 shows a representation of an engineering curve and areas that will be tested.

Figure 5. Engineering Curve took from The Science and Engineering of Materials by Aswkeland, 1994, p. 137

Figure 6 shows the mold the researcher will use and it is referred to as a dog bone: Per ASTM standard.

Figure 6. Dog Bone specimen retrieved from Shimadzu Excellence in Science

The test is implemented through what is commonly known as a pull test.  A specimen called a “dumbbell” or “dog bone” is used to conduct this test in which the specimen is placed in a universal machine. There are grips which attach to the specimen and place tension that is implemented from pulling or tension until the specimen fails. Figure 7 shows how the ASTM D638 will be carried out in the universal testing machine.

Figure 7. Pull test diagram taken from The Science and Engineering of Materials by Aswkeland, 1994, p. 136

The test specimen that was used in this experiment was a specimen shape “I” which has a thickness of 7mm (0.28 in) or less (Standard, A. S. T. M, 2010). The testing machine was setup up for a full figure specimen, hence specimen shape “I” was used. The dog bone specimen specifications can be found in the ASTM Designation: D638 – 14. ASTM D638 is a standard test used for testing the tensile properties of plastic or any other material that has a thickness up to 14mm. ASTM D638 is created by the ASTM and operates at international levels while implementing 12,000 other standards used in several applications. D638 evaluates several tensile properties that are tested to this specification that includes:  modulus, yield strength, ultimate tensile strength, Poisson’s ratio, elongation to failure and reduction of area, which disclose critical material properties.

The dog bone was imported as a DWG file that can be used on the laser machine. The next step involved the researcher purchasing a ¼” thick section of OSB board, which is was used as a test specimen to test against the fiber composite boards. Because the thickness of the dog bone that was tested had to be 1/8” thick, the researcher sanded down the OSB board to achieve this thickness, which was checked with a digital caliber. The researcher, achieved this thickness using a planner, starting off at a thickness of ¼” the OSB was processed through the planner. This was repeated adjusting the height of the blades on the planner gradually until the desired 1/8” was achieved.

Next, the researcher set up the laser cutter to cut the dog bones using the 1/8” thick OSB board. The researcher cut out five dog bones that were used to test and afterward collected the data and recorded the mean, median, and mode and compared the charts and curves of the data that were provided after the test had concluded. The piece OSB was measured and the dimensions entered to ensure the laser had the correct paths to take when cutting and ensure the templates were cut out in the heart of the material. The laser machine used by the researcher was a Boss Laser Model No: LS-2436. The laser was set up in millimeters, which was taken into consideration when measuring the material as mentioned above. The templates were cut at 60% power and a speed of 60 RPM’s in three passes. The power and speed settings were used to ensure that the material was not burned, therefore breaking down the composition and the material. These parameters can vary depending on the machine that is used.

Using the same template of the dog bone loaded into the machine from earlier, the researcher cut the dog bone to test the fiber composite boards. The same power settings were used to cut out the dog bones as used to cut out the OSB board dog bones.

The next step was testing the dog bones made within the testing facility. The machine used for testing the materials conducted several standardized tests. The test conducted consisted of yield strength, tensile strength, breaking strength, and modulus of elasticity. The data was collected from the different dog bones and saved to later show if the tests revealed a significant difference when compared.

3.4 Testing Conditions

The conditions that the test was conducted used the standards and testing of the engineering curve. The formula for this is Sigma=F/A which were used within the stress-strain diagram. The test also yielded tensile strength, yield strength, breaking strength, and modulus of elasticity. The dog bones that were created in the beginning of the research are the specimens used in which to conduct these tests. Using the ASTM D638 testing standard, a constant amount of pulling force was applied to the dog bone to determine the failure point. Once a failure point had been achieved that provides the best performance data, the rate of force was then applied to all specimens of dog bones to collect data.

3.5 Testing Procedures

The testing procedures were based on the guidelines used to test plastics within engineering from ASTM, Standard Test Method for Tensile Properties of Plastics. “This standard is issued under the fixed designation D638; the number immediately following the designation indicates the year of original adoption or, in the case of revision, the year of last revision. A number in parentheses indicates the year of last reapproval. A superscript epsilon (´) indicates an editorial change since the last revision or reapproval. “This standard has been approved for use by agencies of the U.S. Department of Defense” (Standard, A. S. T. M., 2010, p.46).

During the test, the researcher was testing for yield strength, tensile strength, breaking strength and modulus of elasticity. Data was gathered from the engineering curve stress-strain diagram and analyzed to see how the OSB board compares to the fiberboard across all fields. The stress diagram is a curve which shows the amount of stress a material is subjected to. The corresponding axis on the graph is vertical axis stress and the horizontal axis strain. At certain points along this curve, certain aspects were tested and data was collected such as proportional limit, elastic limit, yield point, ultimate stress point, and breaking point.

Proportional limit is a point on the curve up to which the value of stress and strain remains proportional. Elastic limit is the limiting value of stress up to which the material is perfectly elastic. Yield stress is defined as the stress after which material extension takes place more quickly with no or little increase in load. Ultimate stress point is the maximum strength that material have to bear stress before breaking. Breaking point or breaking stress is point where strength of material breaks. (Asfar, 2014, Stress Strain Curve Explanation, para. 1-5)

Using these specific points on the stress diagram, the engineering curve showed specific data associated with each of the limits of the material.

3.6 Data Sources

Data was collected from the ASTM D638 standardized test conducted on the dog bone specimens composed of fiber composite and OSB board. The data was collected from displays that show all the calculations including tensile strength, elongation at break, nominal strain at break, modulus of elasticity. Charts and tables were used to compare the data to project comparisons and differences among the specimens.

3.7 Specific Measures for Success

Looking at the data of each of the specimens and comparing them based on the four categories they were tested will determine if there is a significant difference. The researcher used an independent T-test with a power of 0.05. The T-test was ran on the comparison of the specimens in each of the categories: peak load, peak stress, strain at break, and modulus of GPa. Once the test was ran data was collected and placed in a table in which the P (T<=t) two-tail value was observed. If this value is less than the P-value of 0.05, the test will show a significant difference in the two specimens. Testing the measure of success was valid for this experiment if the hemp specimens surpass data of OSB specimens in three of the four areas tested.

3.8 Threats to Validity

There were some threats to validity when conducting this experiment: Possibilities of air pockets being created when compressing the fibers. Air pockets could create a weakness within the fiber composite board that can cause failure in that specific area. Resurfacing of faces of the digital fabricated molds when they are released being incomplete due to air pockets or lack of complete compression of fibers. The fibers can fail to be completely pressed into complicated areas of the mold causing additional forming when released. Saturation of fibers being in mold adhering to other fibers being separately placed in mold. The fibers cannot all be placed within the mold at one complete time, meaning the fibers will have to be separated at some point to be properly placed in mold. This can allow for space between the fibers and if compression is not successful, then fibers could potentially not adhere to each other. Connection of digital molds to other components of architecture structure weakling mold at those connection points. Depending on the type of connecting to the specific point architecture, the process could weaken the molds to be added.

3.9 Summary

Referring to the pilot work as a guide to conduct the study needed for this research, the researcher should be able to reproduce the research. Using the standard test ASTM D638 and gathering data from the stress diagram the data collected should result in findings that hemp fibers are a sustainable substitute for a material to use in digital fabrication for contemporary architecture.

CHAPTER 4: REVIEWING OF COLLECTED DATA

4.1 Preparation for Data Collection

The researcher conducted the experiment with five dog bone specimens of each material and carefully collected the data of each specimen that was tested.  The pull test was conducted in a lab setting under the supervision of a trained personnel. The test was conducted at rates of 10 samples per second and a pulling rate of 1 mm per minute. A sample test was conducted to ensure that the test would not exceed the pulling capacity load that the machine was set up for and skew the data that would be collected. Each of the specimens was carefully measured using proper measuring tools. A digital caliper was used to measure the width of the testing area of the specimens and a digital thickness gauge to measure the thickness of each specimen. The researcher labeled each of the specimens one through five depending on the material of the dog bone. The following table shows the thickness and width of each specimen.

Figure 8. Thickness and width of specimens (measurements are in inches)

Due to the orientation in which the fibers were laying in the specimens, the results was a difference in variations of thickness.

After the measurements were recorded, the test was conducted on each specimen and data was collected after the specimen reached its breaking point.  The graphs will show the data across the x-axis (Strain in/in) and the y-axis (Stress kPa) which will reveal different data points to observe the behavior of the material. Raw data was collected as well as the graph of the test to show values of characteristics of material at certain points during the test.

4.2 Hemp Fiber Data

Testing on hemp fibers was conducted first and in reference to the labeled specimens indicated by the number. The first specimen test running time was 01:19. The specimen 1 resulted in a peak load (lbf) 43.64, peak stress (lbfin2) of 577.5, strain at break (%) of .579 and a Modulus (GPa) of 1.095. Figure 9 shows the graph of the test which was recorded for specimen 1.

Figure 9. Graph of Hemp specimen 1

The second specimen test running time was 02:27. The specimen 2 resulted in a peak load (lbf) 71.818, peak stress (lbfin2) of 1076.5, strain at break (%) of .809 and a Modulus (GPa) of 1.376. Figure 10 shows the graph of the test which was recorded for specimen 2.

Figure 10. Graph of Hemp specimen 2

The third specimen test running time did not record. The specimen 3 resulted in a peak load (lbf) 69.959, peak stress (lbfin2) of 1010.6, strain at break (%) of .493 and a Modulus (GPa) of 2.233. Figure 11 shows the graph of the test which was recorded for specimen 3.

Figure 11. Graph of Hemp specimen 3

The fourth specimen test running time did not record. The specimen 4 resulted in a peak load (lbf) 73.121, peak stress (lbfin2) of 1141.6, strain at break (%) of .850 and a Modulus (GPa) of 1.974. Figure 12 shows the graph of the test which was recorded for specimen 4.

Figure 12. Graph of Hemp specimen 4

The fifth specimen test running time did not record. The specimen 5 resulted in a peak load (lbf) 83.660, peak stress (lbfin2) of 1237.7, strain at break (%) of 1.007 and a Modulus (GPa) of 1.692. Figure 13 shows the graph of the test which was recorded for specimen 5.

Figure 13. Graph of Hemp specimen 5

The data collected for the hemp specimens revealed that the hemp specimens are able to withstand an average load of 68.4396 lbf before failure or deformation. The hemp fibers on average revealed a peak stress of 1008.78 (lbfin2)   before areas of the fibers began to fail due to force being applied on the dog bone. The hemp fibers on average revealed a strain at break of 0.7476 %, which is also known as elongation of break where the material showed a ratio of length and a preliminary length. The hemp fibers also revealed an average Modulus (GPa) of 1.674, which states the average strength of the cross section by the ratio of stress and strain being applied to the specimen. Specimen five yielded the best numbers in average load, peak stress, and strain at break, but averaged third in Modulus rating. Specimen two had the highest Modulus rating of 2.233, but had overall lowest strain at break of 0.493 %. This collected data will be compared to the data that will be collected form the OSB specimens.

4.3 OSB Board Data

Testing on OSB board specimens was conducted second and in reference to the labeled specimens indicated by the number. The first specimen test running time did not record. The specimen 1 resulted in a peak load (lbf) 43.237, peak stress (lbfin2) of 695.2, strain at break (%) of .0.350 and a Modulus (GPa) of 1.933. Figure 18 shows the graph of the test which was recorded for specimen 1. In the testing of the OSB specimen, the testing resulted in slippage during the beginning of the test which is shown by the erratic lines in the graph.

Figure 14. Graph of OSB specimen 1

The second specimen test running time did not record. The specimen 2 resulted in a peak load (lbf) 58.574, peak stress (lbfin2) of 950.9, strain at break (%) of 0.611 and a Modulus (GPa) of 0.492. Figure 15 will show the graph of the test which was recorded for specimen 2.

Figure 15. Graph of OSB specimen 2

The third specimen test running time did not record. The specimen 3 resulted in a peak load (lbf) 16.168, peak stress (lbfin2) of 258.9, strain at break (%) of 0.489 and a Modulus (GPa) of 0.493. Figure 16 will show the graph of the test which was recorded for specimen 3.

Figure 16. Graph of OSB specimen 3

The fourth specimen test running time did not record. The specimen 4 resulted in a peak load (lbf) 54.947, peak stress (lbfin2) of 841.5, strain at break (%) of 0.403 and a Modulus (GPa) of 1.696. Figure 17 will show the graph of the test which was recorded for specimen 4.

Figure 17. Graph of OSB specimen 4

The fifth specimen test running time did not record. The specimen 5 resulted in a peak load (lbf) 43.234, peak stress (lbfin2) of 668.8, strain at break (%) of 0.420 and a Modulus (GPa) of 1.364. Figure 18 will show the graph of the test which was recorded for specimen 5.

Figure 18. Graph of OSB specimen 5

The data collected for the OSB specimens revealed that the OSB specimens are able to withstand an average load of 43.232 lbf before failure or deformation. The hemp fibers on average revealed a peak stress of 683.06 (lbfin2)   before areas of the fibers began to fail due to force being applied on the dog bone. The hemp fibers on average revealed a strain at break of 0.4546 %, which is also known as elongation of break where the material showed a ratio of length and a preliminary length. The hemp fibers also revealed an average Modulus (GPa) of 1.1956, which states the average strength of the cross section by the ratio of stress and strain being applied to the specimen. Specimen two yielded the best numbers on average load, peak stress, and strain at break, but averaged fifth in Modulus rating. Specimen one had the highest Modulus rating of 1.933, but also had overall lowest strain at break of 0.35 %. This collected data will be compared to the data that was collected form the hemp fiber specimens.

4.4 Comparison of Combined Data Averages

Referring back to the specific measure of success, the researcher was looking for at least three of the sampled areas within the test to provide a 10% increase over OSB in areas specifically tested in order for the research to be successful. Comparing the hemp fiber specimen data to the OSB specimen data the researcher was able to conclude that the hemp fiber specimens are actually a better material to be used over OSB board. The average of the overall data from both tests was used to find the percentage of change in the testing of the materials. The researcher was looking for significantly better results from the hemp fibers.

The calculations for Peak load were68.439643.232-1=0.583, which yielded 58% increase. This was an increase of 25(lbf) in the strength of peak load for hemp over OSB board. The calculations for Peak stress were1008.78683.06-1=0.476, which yielded 48% increase. This was an increase of 326(lbfin2) in strength of peak stress for hemp over OSB board. The calculations for Strain at Break were0.74760.4546-1= 0.644, which yielded 64% increase. This was an increase of 0.29% in strength in break over OSB board. The calculations for Modulus of GPa were1.6741.1956-1=0.400, which yielded 40% increase. This was an increase of 0.478 GPa over OSB board. Figure 19 shows the data between hemp fiber specimen and OSB board specimen along with the increase of data.

Figure 19. Comparison of Data Averages

Using the raw data that was provided by each individual test, the researcher was able to format the data in Excel and make individual comparisons between the specimens according to their labels. The specimen data was used to make individual graphs for each test and then combined to give a visual representation of the test results.

The combined data revealed that the hemp fibers are proven to be more efficient in four of the four categories that were tested by more than the initial 10% specific measures of success.

4.5 Comparison of Data Averages of Individual Specimens

Referring back to the specimens that are labeled by numbers according to the testing, they will be compared to each other individually. This will allow the data to be observed based on the comparison of the specimens instead of an average of the complete data set. The data will be compared in intervals: Hemp specimen 1 to OSB specimen 1, Hemp specimen 2 to OSB specimen 2, and so forth.

The data collected for specimen 1 showed a percentage increase of hemp over OSB. The data is shown on a graph of strain (in/in) over stress (psi). The calculations to convert stress (kPa) to stress (psi) is the Orignal (kPa)/0.0625, 0.0625 being the cross section area of the dog bone 0.125*0.5=0.0625. The strain (in/in) is the Orignal Extensometer in reading/2. Using these formulas, the researcher compiled the data in excel and produced graphs to visualize the data. The percentage increase of hemp over OSB were 698.39673.70-1=0.0366*100=3.66% stress (psi). For strain (in/in) the percentage increase hemp over OSB were 0.00460.0035-1=0.314*100=31.43% strain (in/in). Within the test of specimen one OSB board, the specimens breaking occurred at data entry 795. The break is shown in the graph where the line drops towards the x-axis at 180 degrees. There were five breaks located in specimen 1. Using the peak of the break the researcher was able to locate the data to determine strain (in/in). Figure 20 shows the comparison of the data.

Figure 20. Comparison of Data Specimen 1

The data for specimens two, the percentage increase of hemp over OSB were 1149.08937.18-1=0.226*100=22.6 % stress (psi). For strain (in/in) the increase hemp over OSB were 0.02740.018-1=0.522*100=52% strain in/in.  . Figure 21 shows the comparison of the data.

Figure 21. Comparison of Data Specimen 2

The data for specimens three, the percentage increase of hemp over OSB were 1119.35258.69-1=3.33*100=332.70% stress (psi). For strain (in/in) the percentage increase hemp over OSB were 0.00410.0024-1=0.708*100=70.8% strain (in/in). Within the test of specimen 3 OSB board, the specimens breaking occurred at data entry 194. The break is shown in the graph where the line drops towards the x-axis in 180 degrees. There were three breaks located in specimen four. Using the peak of the first break, the researcher was able to locate the data to determine strain (in/in).  Figure 22 shows the comparison of the data.

Figure 22. Comparison of Data Specimen 3

The data for specimens four, the percentage increase of hemp over OSB were 1169.93879.16-1=0.33*100=33% stress (psi). For strain (in/in) the percentage increase hemp over OSB were 0.0200.011-1=0.818*100=81.8% strain (in/in). Figure 23 shows the comparison of the data.

Figure 23. Comparison of Data Specimen 4

The data for specimens five, the percentage increase of hemp over OSB were 1338.56691.75-1=0.935*100=93.5% stress (psi). For strain (in/in) the percentage increase hemp over OSB were 0.01760.0110-1=0.6*100=60% strain (in/in). Figure 24 shows the comparison of the data.

Figure 24. Comparison of Data Specimen 5

After comparison of the individual data specimens, the researcher was able to conclude that four out of the five stress (psi) proven results of at least a ten percent increase of psi strength of hemp over OSB.  The researcher also concluded that five out of the five strain (in/in) resulted in at least a ten percent increase of in/in strength. The results were as follows: Hemp psi percentage increase over OSB, specimen 1 is 3.66%, specimen 2 is 93.5%, specimen 3 is 33%, specimen 4 is 332.7%, and specimen 5 is 93.5%. Hemp strain (in/in) percentage increase over OSB, specimen 1 is 31.4%, specimen 2 is 60%, specimen 3 is 81.8%, specimen 4 is 70.8%, and specimen 5 is 52%.

Using the data results, the data revealed the ten percent increase needed to confirm specific measures of success.

4.6 Comparison of Data Averages within Categories using T-Test

Looking at the data collected from the pull test conducted on the specimens of each material, the data was arranged in order to conduct a T-test on each individual category in which the samples tested. The data for peak load on each of the five specimens of hemp and OSB were placed as variables within the T-test. Hemp was listed as variable one and OSB listed as variable two. This information was gathered from the following tables listed as Figure 25.

Figure 25. Data information used for performing T-test

After the T-test was conducted the following results were given listed in Figure 26.

Figure 26. T-test on peak load comparison of samples

Looking at the P (T<=t) two-tail value since the test is a two tail-independent test, the value is 0.035324667 which is less than the P-value utilized in the T-test which reveals a significant difference in hemp versus OSB board in peak load.

Looking at the comparison between the hemp and OSB in the category of peak stress the following data was given as shown in figure 27.

Figure 27. T-test on peak stress comparison of samples

The data reveals there is no significant difference in the peak stress of the materials by referencing the P(T<=t) two tail number which is 0.082226529. This number not being less than the P value of 0.05 shows there is no significant difference.

Looking at the next category of strain at the break the following data was given by the T-test as shown in figure 28.

Figure 28. T-test on strain at break comparison of samples

The data reveals that there is a significant difference in the strain at break of the two materials. Looking at the P (T<=t) two-tail data entry the number is 0.030179427. This data entry is less than the P-value of 0.05 which shows a significant difference in the comparison.

The final category that the T-test was performed is the modulus of GPa. The following data was revealed from the T-test as shown in figure 29

Figure 29. T-test on modulus of GPa comparison of samples

The data from the T-test revealed there was no significant difference of the materials in the category modulus of GPa based off of the data for P (T<=t) two tail which is 0.229237892. This data is not less than the P-value of 0.05, therefore, it does not show a significant difference.

Using the T-test and running comparison tests on the four categories individually shows if there is a significant difference when the two materials are compared. Two out of the four tests shows that there is a significant difference, while the other two tests showed there was no significant difference. The researcher was looking for three of the four tests to show a significant difference in order to meet the measure of success for the experiment. The test data shows that there a few reasons in which the data shows the results that were concluded even after the pull test showed promising results. The variance entry data point within the T-test shows high levels of variance. This could be a result of having a low level of specimens that were tested. The researcher only tested five specimens of each material which could have resulted in outliers due to defects within the OSB board. Referring back to figure 25 for the OSB board under peak stress column three the results were 258.9. When compared to the other numbers these numbers are very low in this category. The same conditions apply within the modulus of GPa within the OSB table at entry two and three with the data of 0.492 and 0.493. These numbers are low compared to the other data entries. Using the information referenced from U.S. Patent No. 3,164,511, the possibilities of voids could have been present in the prefabricated OSB board.

The variations of the strands of wood vary within the ranges of the width of an inch to inch and thickness of 0.002 to 0.020 of an inch. Average length sizes range from the lengths between ½” to six inches, any orientation above this causes the erratic proper orientation of the board. (Elmendorf, 1965).

The T-test resulted in a Type-II error which could be concluded due to the number of specimens that were used to conduct the pull test within the experiment. Looking at the areas in which the OSB board showed a dramatic drop in the data points because of possible voids within the material could be a contributing factor. In the future, the research could be conducted again and with an increase in the number of specimens to test, which would show if the OSB board had a void that contributed to the outliers in the experiment.

CHAPTER 5: CONCLUSION

5.1 Conclusion

After the testing of the OSB board and hemp fibers was completed, the researcher could not reach a conclusion based off of the data that was collected. With the data revealing that two of the test areas prove to have a significant increase over OSB board the other two areas of data were inconclusive. The hypothesis of the researcher was also undetermined based off of these findings.  These conclusions were made based off of the information revealed from the data given from the independent two-tail T-tests. Showing significant differences in the test areas of peak load and strain at break, the other two areas peak stress and modulus of GPa are inconclusive. Looking at the variances in these two areas and observing the data collected, the possibilities of outliers are present. Reasons for the outliers can be linked to high levels of the variance and the number of specimens tested. Since the number of specimens used for each material was five for both OSB board and Hemp fiber dog bones, the variances lead the researcher to believe there was not enough data collected from the pull test to eliminate outliers.

Using the information and conducting another experiment, further can be carried out to determine if the hemp fibers are indeed more sustainable for use in the industry over OSB. Using the methods in this research to recreate the experiment and implement 10-15 more test specimens of each material will give a testing area which may produce more sound data to determine a comparison of the two samples.  Recollecting the data and reentering the information to conduct two-tailed T-test should reveal more evidence to the attest the hemp fibers ability for use in industry. If the results determine that the hemp fibers can be used in industry, future works can be conducted on the implementing of hemp fibers into the industry for multiple applications.

5.1 Future Works

Future works in the area of hemp fibers can vary depending on the applications that the hemp fibers would be used for. Using the data from concluded research, fibers show qualities of promising strengths. Applications can be looked at for using hemp fibers in areas of contemporary architecture including structure components. This could result in the replacement of sheathing or drywall, which would increase the green qualities of the building. Increasing the green qualities of the building would promote the building to qualify for LEED (Leadership in Energy and Environmental Design) specifications which lead to environmentally friendly buildings. This can be applied through the implementation of bio green mechanisms within the building's spaces, which are not solely focused on the building components of the buildings alone.

The use of hemp in buildings to help reduce overall loss of items due to fire is another possible area of research. This is another strong suit characteristic of hemp fibers - the ability to withstand fire. Also, the ability of the hemp to resist fire compared to other materials can be substituted in many other applications as well. These applications could include firewalls on vehicles, applications in firefighter suits, cooking materials, and others areas involved with extreme temperatures.

The use of hemp fibers has endless possibilities which could enlighten the world we live in and have little to no impact on the environment. Future research with this material could open these gateways for the impending of hemp use in industry.

LIST OF REFERENCES

About Opendesk (2016) — What is digital fabrication?. In Opendesk.	https://www.opendesk.cc/about/digital-fabrication

Alkbir, M. F. M., Sapuan, S. M., Nuraini, A. A., & Ishak, M. R. (2016). Fibre properties	and crashworthiness parameters of natural fibre-reinforced composite structure: A	literature review. Composite Structures, 148, 59-73.

Arnaud, L., & Gourlay, E. (2012). Experimental study of parameters influencing	mechanical properties of hemp concretes. Construction and building	materials, 28(1), 50-56.

Asfar, J. (2014, September 14). Stress Strain Curve Explanation. In Engineering Intro..	http://www.engineeringintro.com/mechanics-of structures/stress strain curve	explanation

Ash, A. L. (1948). Hemp—production and utilization. Economic Botany, 2(2), 158-169.

Aswkeland, D. (1994). The Science and Engineering of Materials (Third ed., pp.	135	174). Boston: PWS.

Average Annual Precipitation by State (2017). In Current Results Weather and Science	Facts. https://www.currentresults.com/Weather/US/average-annual-state	precipitation.php

Barrett, L. (2014). What is Contemporary Architecture?. In wiseGEEK. 	http://www.wisegeek.org/what-is-contemporary-architecture.htm

Bell, M. (2012). Innovation, Research, Design. In Hemp Architecture. 	http://www.hemparchitecture.com/

Bledzki, A. K., Sperber, V. E., & Faruk, O. (2002). Natural and wood fibre reinforcement	in polymers (Vol. 13). iSmithers Rapra Publishing.

Cherney, J. H., & Small, E. (2016). Industrial Hemp in North America: Production,	Politics and Potential. Agronomy, 6(4), 58.

Dittenber, D. B., & GangaRao, H. V. (2012). Critical review of recent publications on use	of natural composites in infrastructure. Composites Part A: Applied Science and	Manufacturing, 43(8), 1419-1429.

Ehrensing, D.T. (1998) "Feasibility of Industrial Hemp Production in the United States Pacific	Northwest."Oregon State University, Station Bulletin

Elmendorf, A. (1965). U.S. Patent No. 3,164,511. Washington, DC: U.S. Patent and	Trademark Office.

Fortenbery, T. R., & Bennett, M. (2004). Opportunities for commercial hemp production.	Review of agricultural economics, 97-117.

Hemp Fiber (2016). In Hemp Traders.

http://www.hemptraders.com/Hemp-Fiber-s/1828.htm

Krenzler, D.G., T. Petry, B. Nelson, M.J. Anderson, D. Mathern, and R. Todd. Industrial	Hemp as an Alternative Crop in North Dakota: A White Paper Study of the	Markets, Profitability, Processing, Agro- nomics and History. Ag. Econ. Rep.	402, Inst. Nat. Res. Econ. Dev., North Dakota State University,1998.

Kruse, K., Dai, C., & Pielasch, A. (2000). An analysis of strand and horizontal density	distributions in oriented strand board (OSB). European Journal of Wood and	Wood Products, 58(4), 270-277.

Kymäläinen, H. R., & Sjöberg, A. M. (2008). Flax and hemp fibres as raw materials for	thermal insulations. Building and environment, 43(7), 1261-1269.

L. Arnaud, V. Cerezo. 2001. Qualification physique des matériaux de construction à base	de chanvre [Physical Qualification of Construction Materials Based on Hemp]

Li, Z., Wang, X., & Wang, L. (2006). Properties of hemp fibre reinforced concrete	composites. Composites Part A: Applied Science and Manufacturing, 37(3), 497	505.

Mora, E. P. (2007). Life cycle, sustainability and the transcendent quality of building	materials. Building and Environment, 42(3), 1329-1334.

Nguyen, T. T., Picandet, V., Amziane, S., & Baley, C. (2009). Influence of compactness	and hemp hurd characteristics on the mechanical properties of lime and hemp	concrete. European Journal of Environmental and Civil Engineering, 13(9), 1039	1050.

Nusselder, J., & Stijnen, H. M. C. (2006). U.S. Patent Application No. 11/794,333.

Pickering KL et al. Feasibility study for NZ hemp fibre composites. Jadv Mater	2005;37(3):15–20

Plackett D. The natural fiber-polymer composite industry in Europe—technology and	markets. Progress in wood fibre–plastic composite, Toronto, Canada, 2002

Ranalli P., M. Di Candilo, G. Mandolino, G. Grassi & A. Carboni,1999.  Hemp for	sustainable agricultural systems. Agro-Food-Industry Hi-Tech. 2(10): 33–38.

Ranalli, P., & Venturi, G. (2004). Hemp as a raw material for industrial applications.	Euphytica, 140(1), 1-6.

Reas, C., & McWilliams, C. (2010). Form + Code in Design, Art, and Architecture	(pp.9-41). New York, NY: Princeton Architecture Press.

Riedel, U. (1999). Macromolecular Materials and Engineering (Vol. 272, pp. 34-40).	Weinheim,	Germany: Wiley.

Shahzad, Asim.(2012) "Hemp fiber and its composites–a review." Journal of Composite	Materials 46.8	(2012): 973-986.

Shimadzu Corporation. (n.d.). Tensile Test Methods for Plastics: ASTM D638. In	Shimadzu Excellence in Science	.http://www.shimadzu.com/an/industry/petrochemicalchemical/n9j25k00000pyu0	.html

Standard, A. S. T. M. (2010). D638: Standard test method for tensile properties of	plastics. West Conshohocken (PA): ASTM International.

Stevulova, N., Kidalova, L., Cigasova, J., Junak, J., Sicakova, A., & Terpakova, E.	(2013). Lightweight composites containing hemp hurds. Procedia Engineering,	65, 69-74.

Szalapaj, Peter. Contemporary architecture and the digital design process. Routledge,	2014.

Ticoalu, A., Aravinthan, T., & Cardona, F. (2010, November). A review of current	development	in natural fiber composites for structural and infrastructure	applications. In Southern region engineering conference (Vol. 3, pp. 1-5).

Thygesen A., Properties of hemp fibre polymer composites-An optimisation of fibre	properties using novel defibration methods and fibre characterisation, Department	BIO&AFM, The Royal Agricultural and Veterinary University of Denmark, April	2006.

Vignon M. R., Garcia-Jaldon C., Dupeyre D., “Steam explosion of woody hemp	chènevotte”, International Journal of Biological Macromolecules. vol. 17, n° 6,	1995, p. 395-404.

West, D. P. (1998). Hemp & Marijuana: Myths and Realities. The Council.

Zhang, M. Q., Rong, M. Z., & Lu, X. (2005). Fully biodegradable natural fiber	composites from renewable resources: all-plant fiber composites. Composites	Science and Technology, 65(15), 2514-2525.